## Slide 1: Rapid Manufacturing Technologies
Course Instructor
Dr. Senthil Kumar M.
School of Mechanical Engineering (SMEC)
VIT Chennai
Course code: MEE2016

## Slide 2: Text books
I. Gibson l D. W. Rosen l B. Stucker, (2010), Additive Manufacturing Technologies: Rapid Prototyping to Direct Digital Manufacturing, Springer.
Chua C. K., Leong K. F., and Lim C. S., (2003), Rapid Prototyping: Principles and Applications, Second Edition, World Scientific Publishers.
Ma W. and Venuvinod P., Rapid Prototyping and Other Laser based processes, 2004, Kluwer Academic Press.

## Slide 3: Other Reference Books
Peter D. Hilton, Hilton/Jacobs, Paul F. Jacobs, (2000), Rapid Tooling: Technologies and Industrial Applications, CRC Press.
Beaman, J. J. et al., (1997), Solid Freedom Fabrication, Kluwer.
Burns, M., (1993), Automated fabrication, Prentice-Hall.
Liou W. Liou, Frank W. Liou, (2007), Rapid Prototyping and Engineering applications: A Tool Box for Prototype Development, CRC Press.
Ali K. Kamrani, Emad Abouel Nasr, (2006), Rapid Prototyping: Theory and Practice, Springer.
Jacobs, P. F., (1996), Stereolithography and other RP&M technologies, ASME.

## Slide 4: Mode of Evaluation
CAT 1 – 15 marks
CAT 2 – 15 marks
Assignments – (3x10) = 30 marks
FAT exam – 40 marks
Total = 100 marks
****************************
J-Component = 100 marks
Review 1 = 20 marks
Review 2 = 30 marks
Review 3 = 50 marks

## Slide 5: Introduction

## Slide 6: Introduction
Synonyms: Rapid manufacturing technology
Rapid prototyping technology
Solid freeform fabrication
Desktop manufacturing
Layer manufacturing technology
3D Printing
Additive Manufacturing
Notes: Solid Freeform Fabrication is a set of manufacturing processes that are capable of producing complex freeform solid objects directly from a computer model of an object without part-specific tooling or knowledge.

## Slide 7: What is rapid prototyping ?
Rapid prototyping (RP) technologies: It represents all the technologies that can construct three-dimensional physical objects directly from electronic data (CAD data).
Advantage: Builds a prototype in one step, directly from the geometric model of the part to be manufactured.
How does it happen? RP produces components in an additive manner by slicing the 3D-CAD model into a series of discrete layers. These layers are then reconstituted by the RP machine to produce a physical representation of the 3D-CAD model.
Rapid prototyping methods: examples
  Stereolithography (SL)
  Selective laser sintering (SLS)
  3D printing (3DP)

## Slide 8: What is rapid manufacturing?
Rapid Manufacturing (RM):
  rapid manufacturing is the direct production of finished goods using a RP machine that eliminate tooling.
  RM is making functional end products “directly” from CAD using additive technologies.
  It is based on rapid prototyping processes and methods and consist in fast production of functional parts of small series.

## Slide 9: Rapid prototyping/Rapid manufacturing
Notes: Slicing is an essential step in 3D printing that's characterized by the use of software to convert an object model into instructions for a 3D printer. The software essentially slices the object model into multiple layers. Each of these layers are then given values that denote the way in which it should be built.

## Slide 11: Detailed process

## Slide 12: The Generic AM Process
Gibson et al.,

## Slide 13: The Generic AM Process
Step 1: CAD
All AM parts must start from a software model that fully describes the external geometry.
This can involve the use of almost any professional CAD solid modeling software, but the output must be a 3D solid or surface representation.
Reverse engineering equipment (e.g. laser scanning) can also be used to create this representation.
Step 2: Conversion to STL
Nearly every AM machine accepts the STL file format, which has become a standard, and nearly every CAD system can output such a file format.
This file describes the external closed surfaces of the original CAD model and forms the basis for calculation of the slices.

## Slide 14: The Generic AM Process
Step 3: Transfer to AM Machine and STL File Manipulation
The STL file describing the part must be transferred to the AM machine.
Here, there may be some general manipulation of the file so that it has the correct size, position, and orientation for building.
Step 4: Machine Setup
The AM machine must be properly set up prior to the build process.
Such settings would relate to the build parameters like the material constraints, energy source, layer thickness, timings, etc.

## Slide 15: The Generic AM Process
Step 5: Build
Building the part is mainly an automated process and the machine can largely carry on without supervision.
Only superficial monitoring of the machine needs to take place at this time to ensure no errors have taken place like running out of material, power or software glitches, etc.
Step 6: Removal
Once the AM machine has completed the build, the parts must be removed.
This may require interaction with the machine, which may have safety interlocks to ensure for example that the operating temperatures are sufficiently low or that there are no actively moving parts.

## Slide 16: The Generic AM Process
Step 7: Post-processing
Once removed from the machine, parts may require an amount of additional cleaning up before they are ready for use.
Parts may be weak at this stage or they may have supporting features that must be removed.
This therefore often requires time and careful, experienced manual manipulation.
Step 8: Application
Parts may now be ready to be used. However, they may also require additional treatment before they are acceptable for use.
For example, they may require priming and painting to give an acceptable surface texture and finish.
Treatments may be laborious and lengthy if the finishing requirements are very demanding.

## Slide 17: The Generic AM Process
CAD image of a teacup with further images showing the effects of building using
different layer thicknesses

## Slide 18: Historical development of RP and related technologies

## Slide 19: Historical development of RP and related technologies
Reference: Chua C. K., Leong K. F., and Lim C. S., (2003), Rapid Prototyping: Principles and Applications, Second Edition, World Scientific Publishers

## Slide 20: Additive Manufacturing: Need

## Slide 21: Development of rapid prototyping systems

## Slide 22: Rapid prototyping: Need

## Slide 23: Additive Manufacturing Vs. CNC Technology

## Slide 24: Distinction Between AM and CNC Machining
CNC differs mainly in that it is primarily a subtractive rather than additive process, requiring a block of material that must be at least as big as the part that is to be made.
CNC is likely to be a multistage manufacturing process, requiring repositioning or relocation of parts within one machine or use of more than one machine. CNC machines require considerable setup and process planning, particularly as parts become more complex in their geometry.
AM technology can be used to produce a part in a single stage.

## Slide 25: Distinction Between RM and CNC Machining
Material
AM technology was originally developed around polymeric materials, waxes and paper laminates. Subsequently, there has been introduction of composites, metals, and ceramics.
CNC machining is particularly used for hard, relatively brittle materials like steels and other metal alloys to produce high accuracy parts with well defined properties.
Speed
High speed CNC machining can generally remove material much faster than RM machines can add a similar volume of material.
However, RM technology can be used to produce a part in a single stage while CNC machining is usually a multi-stage processing. Hence, Speed must therefore be considered in terms of the whole process rather than just the physical interaction of the part material.

## Slide 26: Distinction Between AM and CNC Machining
Complexity
the higher the geometric complexity, the greater the advantage RM has over CNC.
Accuracy
AM machines generally operate with a resolution of a few tens of microns. It is common for RM machines to also have variable resolution along different orthogonal axes. Typically, the vertical build axis corresponds to layer thickness and this would be of a lower resolution compared with the two axes in the build plane.
The accuracy of CNC machines on the other hand is mainly determined by a similar positioning resolution along all three orthogonal axes and by the diameter of the rotary cutting tools.

## Slide 27: Distinction Between AM and CNC Machining
Geometry
RM machines essentially break up a complex, 3D problem into a series of simple 2D cross-sections with a nominal thickness. In this way, the connection of surfaces in 3D is removed and continuity is determined by how close the proximity of one cross-section is with an adjacent one.
Since this cannot be easily done in CNC, machining of surfaces must normally be generated in 3D space.
Programming
Determining the program sequence for a CNC machine includes tool selection, machine speed settings, approach position, and angle, etc.
In the case of RM, complexity and implications surrounding their choice are minimal in comparison

## Slide 28: Evolution of prototyping systems

## Slide 29: Evolution of prototyping systems
First generation: Manual prototyping
  Traditional (craft-based)
  labor intensive
Second generation: Soft or virtual prototyping (Mid-1970s)
  Application of CAD/CAE/CAM
  Increasing complexity
  Virtual prototype can be stressed, simulated and tested, with exact mechanical and other properties
Third generation: Rapid prototyping (Mid-1980s)
  Solid freeform fabrication/Layer manufacturing
  Benefit of a hard prototype made in a very short turnaround time is its main strong point (relies on CAD modeling)
Reference: Chua C. K., Leong K. F., and Lim C. S., (2003), Rapid Prototyping: Principles and Applications, Second Edition, World Scientific Publishers

## Slide 30: Rapid Prototyping Vs. Virtual Prototyping

## Slide 31: Rapid prototyping vs. Virtual prototyping
Rapid prototyping: The production of a physical model from a computer model without the need of any jig or fixture or NC programming.
Virtual prototyping: The subsequent manipulation of a solid CAD model as a substitute for a physical prototype for the purposes of simulation and analysis, and is not inclusive of the construction of the solid 3D model.

## Slide 32: Virtual prototyping
Virtual prototyping (VP) is the analysis and simulation carried out on a fully developed computer model, therefore performing the same tests as those on the physical prototypes.
It is also sometimes referred to as computer-aided engineering
(CAE) or engineering analysis simulation
Virtual prototyping integrates digital technologies such as computer-aided design (CAD), computer-aided engineering (CAE), and computer-aided manufacturing (CAM) data, into a single visual environment for viewing and analysis.

## Slide 33: Rapid prototyping vs. Virtual prototyping

## Slide 34: Virtual prototyping includes…
Finite element analysis.
Mechanical form, fit and interference checking.
Mechanical simulation.
Virtual reality applications.
Cosmetic modelling.
Assemblability.

## Slide 35: Virtual prototyping: video demo

## Slide 36: Rapid Prototyping: Process Chain

## Slide 37: Rapid prototyping: Process Chain

## Slide 38: Rapid prototyping: Process Chain (continued…)
3D Modeling
  Most time consuming step of the entire process chain
  Interference studies, stress analyses, FEM analysis etc.
Data conversion and transmission
  Conversion CAD data into .STL file format
  Simplest and shortest step of the entire process chain
Checking and preparing
  Defects due to improper modelling and/or file conversion
  Repairing and optimizing 3D models
  Slices the model into cross-sections of thickness ~ 0.12-0.5 mm
Building (mostly automated)
Post-processing (cleaning, post-curing, finishing etc.)

## Slide 39: Rapid prototyping: video demo

## Slide 40: 3D Printing: How it happens?

## Slide 41: Benefits of Rapid Manufacturing Technologies

## Slide 42: Impact of rapid prototyping on product development
Direct benefits…
To the product designers
  Can increase the product complexity
  Need not concern about “manufacturability”
  Can reduce parts count by combining features into a single-piece
  Can minimize material and optimize strength/weight ratios

## Slide 43: …Example:
Light-weight (but complex design) structures are possible due to 3D printing

## Slide 44: …Example:
Light-weight (but complex design) structures are possible due to 3D printing

## Slide 45: …Example:
Light-weight (but complex design) structures are possible due to 3D printing

## Slide 46: …Example:
Light-weight (but complex design) structures are possible due to 3D printing

## Slide 47: …Example:
Light-weight (but complex design) structures are possible due to 3D printing

## Slide 48: …Example:

## Slide 49: By the Numbers: 3-D Printing at Lockheed Martin

## Slide 50: Impact of rapid prototyping on product development (contd..)
Direct benefits…
To the tooling and manufacturing engineer
  The main savings are in costs
  Can realize profits earlier on new products (since fixed costs are lower)
  Assembly of the parts is easy and costs are lower (due to the reduced number of parts)
  Less number of labour required
  Reduced material wastage
  Low inventory costs (Less inventory required)
  General purpose machines can be used (leads to reduction in capital investment)
  Scheduling the production is easy
  Better and easy quality control

## Slide 51: Impact of rapid prototyping on product development
In-direct benefits…
Benefits to Marketing
  Adjust production lot dynamically based on the demand
  No need to project future customer needs/market conditions
  Products meet customer needs more closely
  Can offer the latest technology to the customers
  Can increase the diversity of the product offerings
  Easy to expand and enter into new newer markets

## Slide 52: Impact of rapid prototyping on product development
In-direct benefits…
Benefits to the consumer
  Can buy products which meet individual needs and taste
  Can buy customized products at affordable cost
  Can get products at relatively cheaper rate due to the increased profitability to the manufacturer.

## Slide 53: List of Few Common RP Technologies

## Slide 54: RP Technologies

## Slide 55: Rapid Tooling

## Slide 56: Rapid tooling
Definitions:
Tooling:
  The process of providing a factory with machinery in preparation for production.
  Working or manufacturing aids such as cutting tools, dies, fixtures, gauges, jigs, molds, and patterns of a specialized nature which (unless substantially altered or modified) are limited in use to a specific production line or the performance of a specific contract or job
Rapid tooling:
  The application of rapid prototyping technologies in the preparation of manufacturing tools.
  A process which either uses a rapid prototyping (RP) model as a pattern to create a mold quickly or uses the Rapid Prototyping process directly to fabricate a tool for a limited volume

## Slide 57: Rapid Tooling: Examples

## Slide 58: Rapid Tooling
As Rapid Prototyping (RP) technology becomes more mature, it is beginning to lend itself to other applications such as rapid tooling and rapid manufacturing.
Some traditional tool making methods are considering the use of RP technologies to directly or indirectly fabricate tools.
The Indirect method of rapid tooling (RT) uses the RP pattern as mold.
This is considered as a good alternative to the traditional mold making since it is more efficient and requires less lead-time. This approach is also less expensive and allows for quick validation of designs.
Indirect RT method, the RP process is used for direct fabrication of the tools.

## Slide 59: Rapid Tooling
In summary, rapid tooling is described as a process which uses an RP model as:
a pattern to create mold quickly (e.g. sand casting) or
uses the RP process directly to fabricate a limited volume of tools.
The theme of rapid tooling is the ability to produce multiple copies of a prototype with functional material properties in short lead times.

## Slide 60: Rapid Tooling: Classification

## Slide 61: Rapid tooling (Text book: Chua et al., Page No. 303-)

## Slide 62: Rapid tooling (Text book: Chua et al., Page No. 303-)
Soft tooling
Typically made of silicone rubber, epoxy resins, low melting point alloys and foundry sands
Generally allows for only single casts or for small batch production runs
Hard tooling
Usually made from tool steels
Generally allows for longer production runs
Direct tooling: the tool or die is created directly by the RP process
Indirect methods: Use a pattern obtained by an appropriate RP technique as a model for mould and die making

## Slide 63: Soft tooling

## Slide 64: Example: silicone rubber can be used for soft tooling!

## Slide 65: Applications of Rapid Manufacturing Technologies

## Slide 66: Typical application areas of RP

## Slide 67: Typical application areas of RP

## Slide 68: Applications in Design
CAD Model Verification
  This is the initial objective and strength of RP systems, in that designers often need the physical part to confirm the design that they have created in the CAD system.
  This is especially important for parts or products designed to fulfil aesthetic functions or that are intricately designed to fulfil functional requirements.

## Slide 69: Applications in Design
Visualizing Objects
  Designs created on CAD systems need to be communicated not only amongst designers within the same team, but also to other departments, like manufacturing, and marketing.
  Thus, there is a need to create objects from the CAD designs for visualization so that all these people will be referring to the same object in any communications.
“Many people cannot visualize a part by looking at print. Even engineers and toolmakers who deal with print everyday require several minutes or even hours of studying a print. Unfortunately, many of the people who approve a design (typically senior management, marketing analysts, and customers) have much less ability to understand a design by looking at a drawing.”
-Tom Mueller

## Slide 70: Applications in Design
Proof of Concept
  Proof of concept relates to the adaptation, of specific details to an object environment or aesthetic aspects (such as car telephone in a specific car), or of specific details of the design on the functional performance of a desired task or purpose.

## Slide 71
Marketing and Commercial Applications
  Frequently, the marketing or commercial departments require a physical model for presentation and evaluation purposes, especially for assessment of the project as a whole. The mock-up or presentation model can even be used to produce promotional brochures and related materials for marketing and advertising even before the actual product becomes available.

## Slide 72: Applications in Engineering, Analysis and Planning
Scaling
  RP technology allows easy scaling down (or up) of the size of a model by scaling the original CAD model.
  Example: In a case of designing bottles for perfumes with different holding capacities, the designer can simply scale the CAD model appropriately for the desired capacities

## Slide 73: Applications in Engineering, Analysis and Planning
2. Form and Fit
  Other than dealing with sizes and volumes, forms have to be considered from the aesthetics and functional standpoint as well. How a part fits into a design and its environment are important aspects, which have to be addressed.
  For example, the wing mirror housing for a new car design has to have the form that augments well with the general appearance of the exterior design. This will also include how it fits to the car door. The model will be used to evaluate how it satisfies both aesthetic and functional requirements.
  Form and fit models are used not just in the automotive industries. They can also be used for industries involved in aerospace and others like consumer electronic products and appliances.

## Slide 74: Applications in Engineering, Analysis and Planning
3. Flow Analysis
  Experiments with 3D physical models are frequently required to study product performance in air and liquid flow.
  Such models can be easily built using RP technology.
  Modifications in design can be done on computer and rebuilt for re-testing very much faster than using traditional prototyping methods.
  Flow analyses are also useful for studying the inner sections of inlet manifolds, exhaust pipes, replacement heart valves, or similar products that at times can have rather complex internal geometries.

## Slide 75: Applications in Engineering, Analysis and Planning
4. Stress Analysis
  In stress analysis using mechanical or photo-optical methods or otherwise, physical replicas of the part being analyzed are necessary.
  If the material properties or features of the RP technologies generated objects are similar to those of the actual functional parts, they can be used in these analytical methods to determine the stress distribution of the product.

## Slide 76: Applications in Engineering, Analysis and Planning
5. Mock-Up Parts
  “Mock-up” parts, a term first introduced in the aircraft industry, are used for final testing of different aspects of the parts. Generally, mockup parts are assembled into the complete product and functionally tested at pre-determined conditions, e.g., for fatigue.
  Some RP techniques are able to generate “mock-ups” very quickly to fulfil these functional tests before the design is finalized.

## Slide 77: Applications in Engineering, Analysis and Planning
6. Pre-Production Parts
  The necessary accessory equipment, such as fixtures, chucks, special tools and measurement devices required for the mass-production process are prepared and checked.
  Many of the RP methods are able to quickly produce pilot-production parts, thus helping to shorten the process development time, thereby accelerating the overall time-to-market process.

## Slide 78: Applications in Engineering, Analysis and Planning
7. Diagnostic and Surgical Operation Planning
  In combining engineering prototyping methodologies with surgical procedures, RP models can complement various imaging systems, such as magnetic resonance imaging (MRI) and computed tomography (CT) scanning, to produce anatomical models for diagnostic purposes.
  These RP models can also be used for surgical and reconstruction operation planning.
  This is especially useful in surgical procedures that have to be carried out by different teams of medical specialists and where interdepartmental communication is of essence.

## Slide 79: Applications in Engineering, Analysis and Planning
8. Design and Fabrication of Custom Prosthesis and Implant
  RP can be applied to the design and fabrication of customized prostheses and implants.
  A prosthesis or implant can be made from anatomical data inputs from imaging systems, e.g., laser scanning and computed tomography (CT).
  In cases, such as having to produce ear prostheses, a scan profile can be taken of the good ear to create a computer-mirrored exact replica replacement using RP technology.
  These models can be further refined and processed to create the actual prostheses or implants to be used directly on a patient.
  The ability to efficiently customize and produce such prostheses and implants is important, as standard sizes are not always an ideal fit for the patient.

## Slide 80: General Examples
3D Printed Leg
Human skin created from stem cells using a 3D printer
An example of 3D printing used to create these shoes.
Courtesy: SPI Lasers

## Slide 81: Spread of rapid prototyping by industry worldwide
Courtesy: SPI Lasers